Allchem  SALT TABLETS

Quality certificate

1. Chemical analysis:

NaCl			≥   99,8	  % 			Fe			≤     1 	  mg/kg

H2O 			≤     0,08 %			          Cd			≤     0,05 mg/kg

Parts < 5 mm 	4   %			                      Hg			≤     0,03 mg/kg

Ca			≤   50 	  mg/kg			Pb			≤     1      mg/kg

SO4			≤ 250 	  mg/kg			Sb			≤     1      mg/kg

Mg			≤   20 	  mg/kg			As			≤     2      mg/kg

Cr			≤     2      mg/kg 		           Ni			≤     2      mg/kg

### Se			≤     1      mg/kg		           pH in 1% solution	    6 – 8

K4Fe(CN)6 anticaking 	max  3 ppm			Parts insoluble

in H2O			≤ 150 mg/kg

2. Geometric parameters

Tablets – white color, odourless (round)

Dimensions:

Diameter  		25,00 ± 0,02 mm

Thickness		12,00 ± 0,57 mm

Weight	          11,00 ± 0,4511 g

Density		1,9663 ± 0,1671 g/cm

3. Mechanical strength

Value of push power at the moment of compression of tablet	min	27.040 ± 930 N

Critical value of pressure at the moment of crush of tablet		min	     423 ± 19,0 bar

4. Water solubility

During flow of water with the following parameters:

Temperature			20°  C

Hardness			  7°  n

Flow rate			2,00 dcm3 / h

Concentration of brine	10,00 %

Time of dissolving		73 minutes

As refers European certificates – the producer has: ISO 9001 / 2001, ISO 14001/2004

HACCP / COCEX ALIMENTARIUS

# Text boxes

ADVISE & TRADE CO.

“ K. SKIBINSKI “

Bednarska 9/14

00-310 Warszawa